Section 07840

Firestopping Telecommunications and Data Cabling

PART 1	GENERAL

  - SECTION INCLUDES

- Firestopping of Through Penetrations in Fire Rated Assemblies.

- Smoke Seals.

- Construction enclosing compartmentalized areas.

  - RELATED SECTIONS

- Section 03300 – Cast In Place Concrete: Sleeves and blockouts in concrete assemblies.

- Section 04800 – Masonry Assemblies: Sleeves and blockouts in masonry assemblies.

- Section 07210 – Building Insulation.

- Section 07810 – Applied Fireproofing.

- Section 07900 – Joint Sealers.

- Section 09250 – Gypsum Board.

- Division 16 – Electrical: Electrical work requiring firestopping.

  - REFERENCES

- ASTM E 84, “Surface Burning Characteristics of Building Materials”.

- ASTM E 119, “Fire Tests of Building Construction and Materials”.

- ASTM E 814, “Fire Tests of Penetration Firestop Systems”.

- ANSI/UL263, “Fire Tests of Building Construction and Materials”.

- ANSI/UL723, “Surface Burning Characteristics of Building Materials”.

- ANSI/UL1479, “Fire Tests of Through Penetration Firestops”.

- Underwriters Laboratories Inc. (UL) – Fire Resistance Directory

- National Fire Protection Association (NFPA) – NFPA 101: Life Safety Code.

- National Fire Protection Association (NFPA) – NFPA 70: National Electrical Code.

  - PERFORMANCE REQUIREMENTS

- Fire rated pathway devices shall be the preferred product and shall be installed in all locations where frequent cable moves, add-ons and changes will occur.

- Where non- mechanical products are utilized, provide products that upon curing do no re-emulsify, dissolve, leach, breakdown or otherwise deteriorate over time from exposure to atmospheric moisture, sweating pipes, ponding water or other forms of moisture characteristic during or after construction.

- Where it is not practical to use a mechanical device, openings within floors and walls designed to accommodate telecommunications and data cabling shall be provided with re-enterable products that do not cure or dry.

- Openings for cable trays shall be sealed using re-enterable firestopping pillows.

  - SUBMITTALS

- Submit under provisions of Section 01300.

- Product Data: Provide manufacturer’s standard catalog data for specified products demonstrating compliance with referenced standards and listing numbers of systems in which each product is to be used.

- Shop Drawings: Submit schedule of opening locations and sizes, penetrating items, and required listed design numbers to seal openings to maintain fire resistance ratings.

- Certificates: Product certificates signed by firestop system manufacturer certifying material compliance with applicable code and specified performance characteristics.

- Installation Instructions: Submit manufacturer’s printed installation instructions.

  - QUALITY ASSURANCE

- Products/Systems: Provide firestopping systems that comply with the following requirements:

  - Firestopping tests are performed by a qualified, testing and inspection agency.  A qualified testing and inspection agency is UL, or another agency performing testing and follow-up inspection services for firestop system acceptable to authorities having jurisdiction.

  - Firestopping products bear the classification marking of qualified testing and inspection agency.

- Installer Qualifications: Experience in performing work of this section who is qualified by the firestopping manufacturer as having been provided the necessary training to install firestop products in accordance with specified requirements.

  - DELIVERY, STORAGE, AND HANDLING

- Delivery:

  - Manufacturer’s original, unopened, undamaged containers, identification labels intact identifying product and manufacturer, date of manufacture; lot number; shelf life, if applicable; qualified testing and inspection agency’s classification marking; and mixing instruction for multicomponent products.

  - Handle and store products according to manufacturer’s recommendations published in technical materials.  Leave products wrapped or otherwise protected and under clean and dry storage conditions until required for installation.

B.	Storage and Protection:

1.	Store materials protected from exposure to harmful weather conditions and at temperature and humidity conditions recommended by manufacturer.

  - PROJECT CONDITIONS

- Do not install firestopping products when ambient or substrate temperatures are outside limitations recommended by manufacturer.

- Do not install firestopping products when substrates are wet due to rain, frost, condensation, or other causes.

- Maintain minimum temperature before, during, and for a minimum 3 days after installation of materials.

- Do not use materials that contain flammable solvents.

- Coordinate construction of openings and penetrating items to ensure that through-penetration firestop systems are installed according to specified requirements.

- Coordinate sizing of sleeves, openings, core-drilled holes, or cut openings to accommodate through-penetration firestop systems.

- Schedule installation of firestopping after completion of penetrating item installation but prior to covering or concealing of openings.

PART 2	PRODUCTS

  - MANUFACTURERS

A.	Acceptable Manufacturer: Specified Technologies Inc., 200 Evans Way, Somerville, NJ 08876.  Tel: (800) 992-1180, Fax: (908) 526-9623, Email: specseal@stifirestop.com, Website: www.stifirestop.com.

B.	Substitutions: Not permitted.

C.	Single Source: Obtain firestop systems for each type of penetration and construction condition indicated only from a single manufacturer.

  - MATERIALS

- General: Use only firestopping products that have been tested for specific fire resistance rated construction conditions conforming to construction assembly type, penetrating item type, annular space requirements, and fire rating involved for each separate instance.

- Firestop Sealants: STI SpecSeal® Brand single component latex formulations that upon cure do not re-emulsify during exposure to moisture, the following products are acceptable:

  - Specified Technologies Inc. (STI) SpecSeal® Series SSS Sealant

  - Specified Technologies Inc. (STI) SpecSeal® Series LCI Sealant

- Firestop Putty: STI SpecSeal® Brand intumescent, non-hardening, water resistant putties containing no solvents, inorganic fibers or silicone compounds, the following products are acceptable:

  - Specified Technologies Inc. (STI) SpecSeal® Series SSP Putty

- Firestop Pillows: STI SpecSeal® Brand re-enterable, non-curing, mineral fiber core encapsulated on six sides with intumescent coating contained in a flame retardant poly bag, the following products are acceptable:

  - Specified Technologies Inc. (STI) SpecSeal® Series SSB Pillows

- Fire Rated Cable Pathways: STI EZ-PATH™ Brand device modules comprised of steel raceway with intumescent foam pads allowing 0 to 100 percent cable fill, the following products are acceptable:

  - Specified Technologies Inc. (STI) EZ-PATH™ Fire Rated Pathway

- Firestop Plugs: Re-enterable, foam rubber plug impregnated with intumescent material for use in blank openings and cable sleeves, the following products are acceptable:

  - Specified Technologies, Inc. (STI) SpecSeal Series FP Firestop Plug

PART 3	EXECUTION

  - EXAMINATION

- Before beginning installation, verify that substrate conditions previously installed under other sections are acceptable for installation of firestopping in accordance with manufacturer’s installation instructions and technical information.

- Surfaces shall be free of dirt, grease, oil, scale, laitance, rust, release agents, water repellants, and any other substances that may inhibit optimum adhesion.

- Provide masking and temporary covering to protect adjacent surfaces.

- Do not proceed until unsatisfactory conditions have been corrected.

  - INSTALLATION

- General: Install through-penetration firestop systems in accordance with Performance Criteria and in accordance with the conditions of testing and classification as specified in the published design.

- Manufacturer’s Instructions: Comply with manufacturer’s instructions for installation of firestopping products.

  - FIELD QUALITY CONTROL

- Inspections: Owner shall engage qualified independent inspection agency to inspect through-penetration firestop systems.

- Keep areas of work accessible until inspection by authorities having jurisdiction.

- Where deficiencies are found, repair firestopping products so they comply with requirements.

  - ADJUSTING AND CLEANING

- Remove equipment, materials, and debris, leaving area in undamaged, clean condition.

- Clean all surfaces adjacent to sealed openings to be free of excess firestopping materials and soiling as work progresses.

  - SCHEDULES:

|  | Concrete Floor | Concrete Wall | Gypsum Board Wall |
| --- | --- | --- | --- |
| Penetrant Type |  |  |  |
| Blank Opening | C-AJ-0100, C-AJ-0101 | C-AJ-0100, C-AJ-101 |  |
| Metal Conduits | C-AJ-1080, C-AJ-1240, C-AJ-1353 | C-AJ-1080, W-J-1098, W-J-1100 | W-L-1049, W-L-1222, W-L-1168 |
| Plastic Conduits/ Raceways | C-AJ-2140, C-AJ-2292 | W-J-2018, W-J-2076 | W-L-2093, W-L-2241 |
| Cables | C-AJ-3214, C-AJ-3231, F-A-3015 | C-AJ-3214, C-AJ-3231, W-J-3098, W-J-3099 | W-L-3218, W-L-3219 |
| Cable Trays | C-AJ-4029 | W-J-4021, W-J-4022, W-J-4033 | W-L-4008, W-L-4029, W-L-4043 |

END OF SECTION

Specified Technologies, Inc. (STI)
200 Evans Way

Somerville, NJ 08876

(800) 992-1180 (Telephone)

(908) 526-9623 (Fax)

www.stifirestop.com (Website)